Technical Data Sheet Product: BETAPRIME™ 5504

Description and Application "All in one" primer for glass/ceramic/plastic substrates used in combination with BETASEAL™ EZI–GUN ®, and BETAMATE™ Polyurethane adhesive sealants.

.

| Technical Data |
| --- |
| Basis | Polyisocyanates |
| Colour | Black |
| Pigments | Carbon Black |
| Density | Approx. 0.93 g/cm3 at 23°C |
| Flash Point | - 10°C (closed cup) |
| Viscosity (DIN-cup 4) | 12 - 17 seconds |

| Processing Temperature | -5°C to + 40°C |
| --- | --- |
| Evaporation Time/Flash-off Time | 2 minutes (at 23°C/50r.H), film should be touch-dry |

| Open time | Max. 3 days (72 hours) at 23°C / 50% RH before the primer needs to be re-applied |
| --- | --- |
| Instruction before Use | Shake container well before opening. Shake container for at least 60 seconds. Steel balls inside container need to be released in order to create good dispersion. Caution: the product is extremely hygroscopic! Close containers immediately after use in order to preserve remaining contents If the primer is not contaminated by double dipping or left open, the open shelf life of the primer will be 14 days. |
| Bonding Surface Preparation | All bonding surfaces must be free of silicon, dirt, dust, water, oil, and grease. For cleaning laminated windscreens we would recommend the use of Betabrade F1, in conjunction with Ezi - Clean Surface Preparation Cleaner. |
| Processing Equipment | Quality Felt Applicators |

| Shelf Life | 9 month at 5°C to +25°C in unopened containers (see “use before” date printed on container). |
| --- | --- |
| Shelf Life after Opening | Depending on ambient condition and working method. DIN 4 cup viscosity values must not exceed 17 seconds. |
| Available Containers | 125ml bottles. |
| Protection measures | See health and safety data sheet. |

Dow Automotive Quality Assurance Quality is our utmost goal. Dow Automotive works according to a modern quality management system conforming to ISO/TS 16949:2002. Environment: All sites of Dow Automotive are conforming to ISO 14001:2004. All statements, technical information and recommendations contained in this document are based on tests that we believe are reliable. However,the accuracy or completeness of the statements, information and recommendations is not guaranteed, as before using, the user should determine the suitability of the product for user’s intended purpose. This This document does not create any liability and all warranties, express or implied, including the implied warranties of merchantability and fitness for a particular purpose are disclaimed. Neither seller nor manufacturer shall be liable either in contract or tort for any loss or damage, direct, incidental, or consequential, arising out of the use and or the inability to use the product. Seller’s/manufacturer’s only obligation is the replacement of defective product.