# Technical Data Sheet ## Product: BetasealTM Ezi-Gun®

Description and Application Betaseal™ Ezi-Gun® is a one-component, medium-viscous, humidity-curing polyurethane bonding/sealing compound for direct glazing with fast link up properties and short drive away time. In addition, it has a high shear modulus, very high volume resistivity and good high-frequency properties. Due to these characteristics of Betaseal Ezi–Gun®, a higher body stiffness and full compatibility to glass-integrated antennas can be achieved. It must be used in combination with the appropriate pretreatment system. Please contact your Laddaw® representative for more detailed information.

.

| Technical Data |  |
| --- | --- |
| ## Basis | ## Urethane Prepolymer |
| ## Colour | ## Black |
| ## Density | ## Approx. 1.30 g/cm3 at 23°C |
| ## Flash Point | ## > 100°C |

| ## Environmental temperature at application (Operating Window) | ## -5°C to + 40°C |
| --- | --- |
| ## Temperature range | ## -5°C to + 50°C (unheated) or 50°C to + 80°C (heated) |
| ## Solid Content | ## > 95 % |

| ## Working Time | ## Approx. 15 minutes at 23°C/50% rel. Humidity |
| --- | --- |
| ## Safe Drive Away Time | ## 2 Airbags: ## 90 minutes unheated ## 60 minutes if heated above 50°C ## 1 Airbag: ## 45 minutes unheated or heated (throughout operating window of -5°C to + 40°C) |

| ## Sagging Behaviour | ## Very good |
| --- | --- |
| ## Cure Rate | ## Approx. 3.4 mm in 24 hours at 23°C/50% rel. Humidity |
| ## Ultimate Tensile Strength ## (DIN 53 504) | ## > 5 MPa |
| ## Percentage Elongation | ## > 300 % |
| ## Lap Shear Resistance ## (EN 1465) | ## > 5 MPa (Height of Adhesive Layer: 2 mm) |
| ## G-Modulus | ## Approx. 2 MPa at 10% strain of cured material |
| ## Shore A Hardness ## (DIN 53 505) | ## Approx. 60 |
| ## Specific Electrical Volume Resistivity ## (DIN IEC 93 / VDE 0303 / HD429 S1) | ## 1 x 109 Ωcm |
| ## Abrasion Resistance | ## High |

| ## Temperature Stability (of cured material) | ## - 40°C to + 100°C |
| --- | --- |
| ## Resistance to Chemicals | ## Highly resistant to aqueous chemicals, petrol, alcohol and mineral oils. Conditionally resistant to esters, ketones, aromatics and chlorinated hydrocarbons |
| ## Bonding surface preparation | ## All bonding surfaces must be free of silicon, dirt, dust, water, oil, and grease. Priming is required prior to application, unless bonding to freshly cut-back polyurethane. |

| ## Processing equipment | ## Hand, battery and pneumatic equipment |
| --- | --- |
| ## Cleaning | ## Uncured Betaseal residues can easily be removed with BETACLEAN 3500. Hardened Betaseal residues can only be removed mechanically. |
| ## Shelf life | ## Short time storage temperature: -5°C to +40°C ## 9 Months (at 5°C to +25°C in unopened containers) ## See "use before" date printed on container. |

| ## Containers | ## 400 ml sausages. |
| --- | --- |
| ## Protection measures | ## See health and safety data sheet. |

Dow Automotive Quality Assurance ## Quality is our utmost goal. Dow Automotive works according to a modern quality management system conforming to ISO/TS 16949:2002. ## Environment: All sites of Dow Automotive are conforming to ISO 14001:2004. ## All statements, technical information and recommendations contained in this document are based on tests that we believe are reliable. ## However, the accuracy or completeness of the statements, information and recommendations is not guaranteed, as before using, the user should determine the suitability of the product for user’s intended purpose. ## This document does not create any liability and all warranties, express or implied, including the implied warranties of merchantability and fitness for a particular purpose are disclaimed. Neither seller nor manufacturer shall be liable either in contract or tort for any loss or damage, direct, incidental, or consequential, arising out of the use and or the inability to use the product. Seller’s/manufacturer’s only obligation is the replacement of defective product.